| Faculty | Electrical Engineering and Computer Sciences |
| --- | --- |
| Course Title | Material Science (MSC) |
| Number of ECTS credits | 6 |
| Hours per week (SWS) | 4 |
| Semester | Master / Winter semester |
| Course objective | This module provides specific knowledge of materials science needed in the field of microelectronics and microsystem engineering. Key aspects are semiconductor physics, thin films and material properties important for microsystem applications. Special aspects are reinforced in laboratory experiments After completion of this course the students are able to • understand the physical concept leading to different kinds of solids • apply the concept of entropy to different applications like phase diagrams, crystalline imperfections and ordered states • work with phase diagrams • derive semiconductor properties from band model • dimension of materials for microsystem applications • identify the influence of deposition parameters on materials properties of thin films • conduct, interpret and document experiments in a scientific way |
| Prerequisites | No specific pre-condtions |
| Recommended reading | W. D. Callister, Materials Science and Engineering: An Introduction, Wiley, 2014 |
| Teaching methods | Tuition in seminars (2 SWS), laboratory exercises and projects (2 SWS) |
| Assessment methods | Oral examination (30 min) or written work under supervision (90 min) and scientific experimental work |
| Language of instruction | English |
| Name of lecturer | Prof. Dr. rer.nat. Ludger Kempen |
| Email | Ludger.Kempen@hs-bremen.de |
| Link | http://www.hs-bremen.de/internet/de/studium/stg/mscee/ |
| Course content | • Atoms and bonding • Structure of solids • Influence of imperfections on crystalline solids • Entropy, thermal equilibrium and kinetics • Diffusion in solids • Phase diagrams • Conductivity and band model of solids • Dielectric, magnetic and optical properties • Deposition techniques and properties of thin films |